| Component - Plastics | E351522 |
| --- | --- |
| DONGGUAN QILONG ELECTRICITY CO LTD |  |
| YEWU INDUSTRIAL DISTRICT MEILIN, DALINGCHAN TOWN, DONGGUAN GUANGDONG 523820 CN |  |
| QL80A |  |
| Polyvinylchloride (PVC), furnished as pellets |  |

|  | Min Thk | Flame |  |  | RTI | RTI | RTI |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Color | (mm) | Class | HWI | HAI | Elec | Imp | Str |
| BK, WT | 1.5 | V-0 | - | - | 50 | 50 | 50 |
|  | 3.0 | V-0 | - | - | 50 | 50 | 50 |

| Comparative Tracking Index (CTI): | - | Inclined Plane Tracking (IPT): | - |
| --- | --- | --- | --- |
| Dielectric Strength (kV/mm): | - | Volume Resistivity (10x ohm-cm) : | - |
| High-Voltage Arc Tracking Rate (HVTR): | - | High Volt, Low Current Arc Resis (D495): | - |
| Dimensional Stability (%): | - |  |  |

ANSI/UL 94 small-scale test data does not pertain to building materials, furnishings and related contents. ANSI/UL 94 small-scale test data is intended solely for determining the flammability of plastic materials used in the components and parts of end-product devices and appliances, where the acceptability of the combination is determined by UL.

| Report Date: 2012-06-08 Last Revised: 2012-06-08 | © 2012 UL LLC |  |
| --- | --- | --- |

IEC and ISO Test Methods

|  |  |  | Thickness |  |
| --- | --- | --- | --- | --- |
| Test Name | Test Method | Units | Tested (mm) | Value |
| Flammability | IEC 60695-11-10 | Class (color) | 1.5 | V-0 (BK, WT) |
|  |  |  | 3.0 | V-0 (BK, WT) |
| Glow-Wire Flammability (GWFI) | IEC 60695-2-12 | C | - | - |
| Glow-Wire Ignition (GWIT) | IEC 60695-2-13 | C | - | - |
| IEC Comparative Tracking Index | IEC 60112 | Volts (Max) | - | - |
| IEC Ball Pressure | IEC 60695-10-2 | C | - | - |
| ISO Heat Deflection (1.80 MPa) | ISO 75-2 | C | - | - |
| ISO Tensile Strength | ISO 527-2 | MPa | - | - |
| ISO Flexural Strength | ISO 178 | MPa | - | - |
| ISO Tensile Impact | ISO 8256 | kJ/m2 | - | - |
| ISO Izod Impact | ISO 180 | kJ/m2 | - | - |
| ISO Charpy Impact | ISO 179-2 | kJ/m2 | - | - |

© 2012 UL LLC

- UL Online Certifications Directory

Home Quick Guide Contact Us UL.com

- QMFZ2.E351522 Plastics - Component

Additional information regarding this certification can be found in UL's iQ Family of Databases (iq.ul.com).

For additional information concerning the individual material, click on the material designation.

Page Bottom

Plastics - Component

| See General Information for Plastics - Component |  |  |
| --- | --- | --- |
| DONGGUAN QILONG ELECTRICITY CO LTD | E351522 |  |
| YEWU INDUSTRIAL DISTRICT MEILIN |  |  |
| DALINGCHAN TOWN |  |  |
| DONGGUAN, GUANGDONG 523820 CHINA |  |  |

|  |  |  |  |  |  |  |  |  | H | D |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Min. |  | H | H | R T I |  |  | V | 4 | C |
|  |  | Thk | Flame | W | A | Elec | Mech |  | T | 9 | T |
| Material Dsg | Color | mm | Class | I | I |  | Imp | Str | R | 5 | I |
| Polyvinylchloride (PVC), furnished as pellets. |  |  |  |  |  |  |  |  |  |  |  |
| QL80A | BK, WT | 1.5 | V-0 | - | - | 50 | 50 | 50 | - | - | - |
|  |  | 3.0 | V-0 | - | - | 50 | 50 | 50 |  |  |  |

Marking: Company name and material designation on container, wrapper or finished part.

| Last Updated on 2012-06-08 |  |  |  |
| --- | --- | --- | --- |
| Questions? | Print this page | Terms of Use | Page Top |

?2012 UL LLC

When the UL Leaf Mark is on the product, or when the word "Environment" is included in the UL Mark, please search the UL Environment database for additional information regarding this product's certification.

The appearance of a company's name or product in this database does not in itself assure that products so identified have been manufactured under UL's Follow-Up Service. Only those products bearing the UL Mark should be considered to be Listed and covered under UL's Follow-Up Service. Always look for the Mark on the product.

UL permits the reproduction of the material contained in the Online Certification Directory subject to the following conditions: 1. The Guide Information, Designs and/or Listings (files) must be presented in their entirety and in a non-misleading manner, without any manipulation of the data (or drawings). 2. The statement "Reprinted from the Online Certifications Directory with permission from UL" must appear adjacent to the extracted material. In addition, the reprinted material must include a copyright notice in the following format: "© 2012 UL LLC".